## Slide 1
PDFgui: quick start

## Slide 2: Installing PDFgui
Go to diffpy.org
Select pdfgui from the “Products” dropdown
Follow the instructions
  If you don’t have Anaconda installed I recommend installing miniconda
If all else fails, install the windows executable version instead (diffpy-1.0-r3067.exe)

## Slide 3: Running PDFgui
Open a terminal
  E.g., type cmd into the search box on Windows
  “cd” to where you are working
    E.g., cd scratch/toscaland21

## Slide 4: Installing structure viewer if you like
Download Vesta (or another preferred viewer)
  Google for “vesta structure viewer” and select “download”
  Download and extract the files, maybe to the programs directory or your computer
  In PDFgui,
    Edit -> preferences
    Browse for the vestaXXX.exe file in your extracted download file
    Click OK

## Slide 5: Basic rules of PDFgui usage
Join diffpy-users Google group and ask questions there
  Do it now! Google for diffpy-users and request to join
Every time you are in a happy-place, save your work into a project file (ctl-s)
  This will save you a lot of time if (as sometimes happens) PDF gets stuck and has to be restarted.
  Remember “ctl-s”

## Slide 6: Workflow
Fits -> New fit, give it a name if you like
Select the fit
Data -> new data set
  Browse for data file
If you have a cif file
  Phases -> browse for the cif file
If you don’t have a cif yet
  Pdfitc.org -> structuremining
    Upload the pdf file and give as much info as you have about composition
    Download your preferred result and extract the files
    In pdfgui, browse for the cif file and select it

## Slide 7: Some suggestions
Sanity checks
  Plot your data, does it look ok?
  Calculate your model before doing a full refinement and plot it, does it look ok, as you expect?
  Check you refinement results, are the numbers ok? A good fit doesn’t necessarily mean a good model!
  Check to see if refined parameters are highly correlated (>90%). It means that their refined numbers will be somewhat uncertain
  SAVE YOUR PROJECT FREQUENTLY!

## Slide 8
PDFgui: Layout
Tabs to panes
The layout can be somewhat customized to create comfortable work environment

## Slide 9
Creating a simple fit using a preexisting structure file
Appearance of a PDFgui window after a PDF dataset is loaded.

## Slide 10
Creating a simple fit using a preexisting structure file
Adjusting data set related configuration.

## Slide 11
Creating a simple fit using a preexisting structure file
Setting up the refinement parameters and constraints: experimental parameters

## Slide 12
Creating a simple fit using a preexisting structure file
Setting up the refinement parameters and constraints: model structure

## Slide 13
Creating a simple fit using a preexisting structure file
Reviewing the fit parameters and conditions

## Slide 14
Creating a simple fit using a preexisting structure file
The refinement progress is displayed in the PDFfit2 Output panel.

## Slide 15
Creating a simple fit using a preexisting structure file
Updating the set of initial values of refined parameters.

## Slide 16
Creating a simple fit using a preexisting structure file
An example of PDFgui plotting capabilities: displaying a fit.

## Slide 17
Creating a simple fit using a preexisting structure file
An example of PDFgui plotting capabilities: displaying a parameter.

## Slide 18
Creating a simple fit using a preexisting structure file
Using “Journal” feature can be a convenient way for taking notes.

## Slide 19
Building structure model using crystal symmetry
Expanding the unit cell using space group information.

## Slide 20
Building structure model using crystal symmetry
Setting up symmetry constraints to be used in a refinement.

## Slide 21
Calculating PDF from a structure
An example of the calculation configuration panel.

## Slide 22
Multistage fitting
Sequential refinement where fits are chronologically linked

## Slide 23
Sequential fitting of incremental r-series
Appearance of the setup panel for specifying an incremental r-series fit conditions.

## Slide 24
Sequential fitting of temperature series
Setting up a T-series sequential refinement for LaMnO3.
Ordering by temperature will ensure that the fits are linked correctly.

## Slide 25
Sequential fitting of temperature series
Displaying refinement results as a function of external parameter: T-series refinement

## Slide 26
Sequential fitting of doping series
Loading of the Ca-doping data series of LaMnO3 system.
Verify that proper doping assignment was carried out!

## Slide 27
Sequential fitting of doping series
Displaying refinement results as a function of external parameter: doping series refinement

## Slide 28
Nanoparticle structure
Fitting the structure of a nanoparticle: 3nm CdSe nanoparticle example

## Slide 29
Displaying the structure
Using AtomEye functionality for 3D visualization of the initial and refined PDF structures structure.

## Slide 30
PDFgui tutorial content
Plan is to cover up to 11 examples covering various aspects of PDFgui functionality
GOALS:
    becoming familiar and comfortable with the program
    building up basic expertise and awareness of various PDFgui capabilities
Examples:
    Ni X-ray and neutron data refinement
    Ni neutron-Xray corefinement
    Ni/Si mixture refinement; phase analysis
    Ni T-dependence sequential refinement
    LaMnO3 T-dependence sequential refinement – complex system example
    LaMnO3 800K data fitting - r-dependent sequential refinement example
    Nanoparticle examples: CeO2 and CdSe systems
    La2CuO4 doping-dependent sequential refinement example

## Slide 31
Live PDFgui Demo (time permitting)